## Slide 1
2024/07/11, 가속기여름학교, 고려대학교
Introduction to Synchrotron Small-angle X-ray Scattering
Tae Joo Shin
Graduate School of Semiconductor Materials and Devices Engineering, Ulsan National Institute of Science and Technology (UNIST)
tjshin@unist.ac.kr

## Slide 2
Table of Contents
Introduction
SAXS beamline
Basics of Small-angle X-ray scattering
Structural Information obtained by SAXS
Applications
Conclusion

## Slide 3
Scattering from Nature - Forest Corona, Pollen Corona
Photo by Till Credner and Sven Kohle
13.5 μm diameter water droplets.
20-30 μm

## Slide 4
Photon (Synchrotron Radiation) interaction with matter

## Slide 5
X-ray scattering/diffraction
Crystal
Fiber
Solution
X-ray
X-ray
X-ray

## Slide 6
SAXS is the universal method for nanostructure analysis
• Sensitive – low concentration (down to 0.1%)
• Noninvasive – no preparation, staining or drying
• In-situ, real-time capabilities
• Extremely versatile (solids, liquids, gas phase)
 Structural information from the scattering patterns?
WAXD
WAXD
Small-/wide-angle X-ray scattering ?
Crystalline sample / homogeneous structure --> Small-angle X-ray diffraction (SAXD)
Solution sample / inhomogeneous structure --> Small-angle X-ray Scattering (SAXS)
Notes: 6

## Slide 7
 In order to get the complete picture you need both!
Electron
Microscopy
Small details are visible
X-ray
Scattering
Small details are NOT visible
Average over large samples are hard to obtain
The results are UNIQUE but NOT representative
Preparation artifacts are inherent
Average over the whole sample is always obtained
The results are REPRESENTATIVE but AMBIGOUS
NO preparation artifacts (in vitro experiments)
Electron Microscopy vs. X-ray Scattering

## Slide 8
SAXS Beamline : ex) 6D UNIST-PAL Beamline
Slit
Ver. : 0.17 mrad
Hor. : 2 mrad
100 μm
Beam size [mm] 4.42 4.6
Beam size [mm] 26 39
CM 13 m
DCM 19.5 m
Sample 36 m
BM source 0 m
100 μm
CCD detector
Wall
FE slit
Bending Magnet
Photon
shutter
DCM
FM
Experimental Hutch
Hutch Shutter
Sample
Aperture pinhole
Optics Hutch
CM (L = 1.2 m)
FM 24 m
Safety shutter
Slit
Hutch Slit
Fixed mask
4 mrad (≈0.229o)
4 mrad (≈0.229o)
Vacuum path
R = 6.8755 m
B = 1.4557 T
WB slit
Rh(5nm)/Pt(30nm)
Rh(5nm)/Pt(30nm)
1,400 mm
Si(111) DCM
Fixed exit
Sagittal focusing
2:1 focusing
(1)
(2)
(3)
(4)
(5)
R(m) ≈ 3.34E(GeV)/B(T)
Ec(keV) ≈ 2.218E3(GeV)/R(m) ≈ 8.7 keV

## Slide 9
SAXS Beamline : instruments, sample stages
solution sample cell
solid sample cell
capillary sample cell
solution sample cell
solution sample cell
solid sample cell
Schematic
Sample cells
Hutch
Sample cells

## Slide 10
Beamline Optics : Mirror
Collimating flat mirror
L = 1.2 m-long Si crystal with Rh(5 nm)/Pt(30 nm) coating
0.17 mrad
3.0 GeV
Focusing mirror: Two-dimensional focusing (toroids and ellipsoids)
Rs = Rm sin2i
Lens formula: 1/f = 1/F1 + 1/F2
Focal length: f = [Rm sin i]/2
 Rm = [2/sin i] [F1·F2/(F1 + F2)]
Ex) i = 4 mrad, F1 = 24 m, F2 = 12 m, then Rm  8 km
Rm
Rs
: sagittal radius
Ex) i = 4 mrad and Rm = 8 km
 Rs = 48 mm
Darwin width
ωD = 2reF(hkl)λ2/πVsin(2θ)
F(hkl) = structure factor
V = volume of unit cell
ex) Si(111) crystal @8 keV --> ωD  40 rad
Δθ = [Δψ2 + ωD2]1/2
170 μrad

## Slide 11
Beamline Components : 3-Slits collimation geometry
Journal of X-Ray Science and Technology 20 (2012) 331–338
3-Slits collimation --> Minimal parasitic scattering
Direct beam size (@detector)
Total beam size including the “diagonal parasitic scattering” contribution (@detector)
Smallest angle free from parasitic scattering
SAXS spatial resolution (maximum dimension resolvable in real space)
Relation between the apertures and the distances among the three slits

## Slide 12
Beamline Components : 3-Slits collimation geometry
3-Slits collimation --> Minimal parasitic scattering
Journal of X-Ray Science and Technology 20 (2012) 331–338

## Slide 13
2-Slits collimation W/ hybrid blade
J. Appl. Cryst. (2008) 41, 1134–1139
Beamline Components : 2-Slits collimation geometry

## Slide 14
sample
2D Detector
Beamstop
with a photodiode
WAXD
sample
SAXS
SAXS & WAXD Geometry
2q = 0.02o ~ 4o
> 0.5 m
(2q = 0.8o ~ 30o)
X-ray
6D UNIST-PAL beamline
X-ray
nl = 2d· sinq

## Slide 15
Solution Small-angle X-ray scattering (Sol-SAXS) ?

## Slide 16
Solution Small-angle X-ray scattering (Sol-SAXS) ?

## Slide 17
+
Scattering by X-ray?
Elastic Scattering
-
-
-
λ1
-
-
-
λ1
λ2
E = hc/λ1
λ1=λ2
Interference of Waves
Constructive interference
Destructive interference

## Slide 18
Scattering by X-ray : interference of secondary waves
Small distance between electrons
 scattering at large angle is intensified
Large distance between electrons
scattering at small angle is intensified

## Slide 19
Interference of Waves
Scattering vector
λ
2θ
Incident Beam :
Scattered Beam :
q
- Scattering vector :
Domain spacing :
- Amplitude of scattered X-ray :
(FT of electron density distribution)
Scattering by X-ray : interference of secondary waves
Incident Beam :
λ
Incident Beam,
2θ
Scattered Beam,

## Slide 20
2π : λ = Δϕ : ΔC

(참고자료) Phase difference (shift), wave displacement
20/57

## Slide 21
(참고자료) Scattering by X-ray
d
c
2q
d
, ω=2πν)
21/57

## Slide 22
At the detector,
For N scatterers,
+const. of (r)
(r): (SLDD, scattering length density distribution)
(참고자료) Scattering by X-ray

## Slide 23
FT
IFT
FT
IFT
Scattering length density
(electron density)
Scattering amplitude
X
Squaring
Autocorrelation
Autocorrelation function
Form factor term
Structure factor term
Scattering intensity
Information from SAXS
Real space
Reciprocal space
X
23/57

## Slide 24
autocorrelation function of (r)
Autocorrelation function
24/57

## Slide 25
Physical meaning of autocorrelation function
(r) is related to the average of (u)(u’),
 (r) specifies how the densities (u) and (u’) in neighboring regions separated by r are correlated to each other on the average.
 Correlation between the electron density distributions at two given positions.
25/57

## Slide 26
Null scattering or scattering at q=0
Experimentally unobservable
=0 (by the definition of (r)
Meaningful only r is of the same order of magnitude as the sample dimension; macroscopic dimension
(): relative electron density
Normalized Autocorrelation function
26/57

## Slide 27
1.
2. Autocorrelation function approach
What determines the strength and pattern of scattering from a sample is not the absolute value of the scattering length density but rather the fluctuations or the heterogeneities in the scattering length density present in the sample. The absolute value of the scattering length density governs the intensity of the null scattering, which is of course unmeasurable and therefore has no practical meaning. If we are to increase the scattered intensity from a sample for case of measurement, we have to increase the contrast in the scattering length density among different molecules, species, or regions in the sample.
*Babinet’s Reciprocity Principle: All produce identical Iobs(q)
Autocorrelation function
27/57

## Slide 28: Correlation functions
Totally disordered system
Amorphous system
Monoatomic liquid or paracrystalline state
Close-packed crystal
28/57

## Slide 29
𝜌(𝑟) & (𝑟) of lamellar structure
Ideal ordering
Long period change
Crystal thickness change

## Slide 30
Pair distance distribution function (PDDF)
30/57

## Slide 31
Particle’s SHAPE
Distribution of distances of atoms from centroid
1D: only distance, not direction
20:1 = qmin : qmax  usually OK
p(r)  alternative measure of Rg and also longest cord
Scattering Intensity & Pair distance distribution function
Core-shell structure
Form factor
PDDF
31/57

## Slide 32
Scattering Intensity & Pair distance distribution function
Scattering Intensity (Form factor)
Pair distance distribution function
Particles
32/57

## Slide 33
Invariant
The invariant Q is defined as the quantity obtained when I(s) is integrated with respect to s throughout the reciprocal space.
An isotropic material for which I(s) depends only on the magnitude of s.
The invariant Q can be regarded as representing the overall scattering powder of the sample that takes into account the intensity of scattering that is expected from it under all possible scattering geometry.
Analyze the size distribution of the sample and the interactions between particles.
33/57

## Slide 34
Fourier Transform (FT)
Courtesy of Byeongdu Lee, APS, ANL (USA)
FT
FT
FT
FT
FT
FT
FT
FT
size
elongation
orientation
distribution
size, orientation
shape
facet
Fourier transform
Real
Imaginary
Real
Imaginary
FT
FT
ρ(r): scattering length density distribution
34/57

## Slide 35
Reciprocal lattice construction
Direction of reciprocal lattice
- a*  (100) plane, b,c-plane of the real lattice
- b*  (010) plane, a,c-plane of the real lattice
Length of reciprocal lattice
- a* : 1/d100
- b* : 1/d010
a
b
x
y
d010
d100
Real lattice (crystal planes)
Reciprocal lattice (diffraction spots)
a*
b*
200
100
000
010
020
030
a*
b*
35/57

## Slide 36
1. limit q  0: Electron density fluctuations
2. Guinier range (0.1<q·Rg<1.3)
: particle size
3. Particle shape, large scale structures
4. Porod range : Particle Surface/volume
5. Intermolecular interaction
Information from SAXS
36/57

## Slide 37
Sphere sample: Scattering intensity from Form factor
37/57

## Slide 38: Spherical Shell sample
38/57

## Slide 39
Radius of gyration, Size distribution
O. Glatter & O. Kratky ed., “Small Angle X-ray Scattering”, Academic Press (1982).
Guinier plot: log (I(q)) vs q2
Size distribution
Gaussian distribution
Distribution ⇧  fringes missing
39/57

## Slide 40: Size: Radius of gyration?
Radius of gyration: Rg
Rg2 is the average squared distance of the scatterers from the centre of the object
Ex)
Rg2 =(12+ 12+ 12+ 22+ 22+ 32 )/6=20/6
Rg=√3.333 = 1.82
2
2
1
1
1
3
Scattering length density
Position vector from centre of mass
40/57

## Slide 41: How to find out Rg : Guinier Law
For q∙Rg < 1.3 (Typically)
Plot lnI vs q2
→ Straight line, slope –/3
→ True for all shapes (but works best for spheres)
Solid sphere radius R: Rg = √(3/5) R
Thin rod length L: Rg = √(1/12) L
Thin disk radius R: Rg = √(1/2) R
Rg for different objects
Guinier Rg → 41.8 Å
in the range
of q∙Rg < 1.3
41/57

## Slide 42
Porod’s law
For a sharp interface, the scattered intensity decreases as q-4.
Combination of Porod’s law & Invariant Q
 important for the characterization of porous materials!
42/57

## Slide 43
Dense System
rij ≈ λ
 interparticle interferences are not negligible
r12
λ
P
I
Structure factor
Form factor
Intensity
43/57

## Slide 44: Dense system: Form factors & Structure Factors
44/57

## Slide 45
SAXS more…
45/57
SAXS
Combined measurements with DSC, viscoelasticity, wide q-range
- Hierarchical structure
- Anisotropic structure
Time-resolved SAXS
- Structure evolution, degration
XPCS
-dynamics
- Structure fluctuation
GI-SAXS
- Thin film, orientation, interface, surface
Microbeam SAXS
- Inhomogeneity of nano-structure
- Small area

## Slide 46
Colloidal System
Biomolecules
Block copolymer
Hydrogel
Polymer Micelle
Conjugated Polymer
Polymer Membrane
Applications
46/57

## Slide 47
1. Block Copolymers : Nanosructure & Phase Behavior
Nano structure | Peak Ratio
Lamellae | 1:2:3:4
Sphere (fcc) | √3:√4:√8:√11:√12 etc.
Sphere (bcc) | √2:√4:√6:√8:√10 etc.
Gyroid | √6:√8:√14:√16:√20 etc.
Double diamond | √2:√3:√4:√6:√8 etc.
Hexagonal | 1:√3:√4:√7:√12 etc.
Peak | Position | Ratio
1st | 0.24 nm-1 | 1
2nd | 0.48 nm-1 | 2
3rd | 0.72 nm-1 | 3
4th | 0.96 nm-1 | 4
Gyroid
Sphere (fcc)
Lamellae
Lamellae
47/57

## Slide 48
2. Micro-beam SAXS
* Low-voltage Actuator
Beam size
- Current : 60 (V) X 450 (H) mm2
- Year 2014 : 20 (V) X 150 (H) mm2
- Future : 8 (V) X 20 (H) mm2
48/57

## Slide 49
3. Colloid study by Rheo-SAXS
Shear Alignment
Shear Aligning
Shear rate (1/sec)
Shear rate (1/sec)
Tangential direction
Radial direction
49/57

## Slide 50
4. Nanostructure during battery cycling: Li-ion Battery (in-operando)
Li-ion Battery In-operando SAXS
meso-Co3O4 electrode
meso-SnO2 electrode
meso-TiO2 electrode
 LiSnO2
50/57

## Slide 51
in-situ Tensile Experiment (Tr-mode)
Linkam Tensile stress testing system
In-situ SAXS & WAXD patterns of PCL
5. Orientation evolution by Tensile Experiment of PCL
51/57

## Slide 52
6. Micro-fiber Structure Analysis (1)
PEDOT-PSS Single Fiber (Dia. 30 μm)
52/57

## Slide 53
6. Micro-fiber Structure Analysis (2)
PEDOT-PSS Single Fiber (Dia. 30 μm)
53/57

## Slide 54
Data analysis software ATSAS 3.2.1
Data analysis : Model Fitting
https://www.embl-hamburg.de/biosaxs/software.html
54/57

## Slide 55
Data analysis : Model Fitting
https://www.nist.gov/ncnr/data-reduction-analysis/sans-software
https://usaxs.xray.aps.anl.gov/software/irena
55/57

## Slide 56
Conclusion
e-
Synchrotron radiation
Synchrotron radiation
Bending Magnet
Electromagnetic radiation (synchrotron radiation) is given off when very high energy charged particles are accelerated.
1. Synchrotron SAXS Beamlines  Various applications
2. SAXS  Structure-Property Relationship  New Material Design & Synthesis
3. in-situ Experiments  Many issues, Operando, Understanding & Process Optimization
Future works : More in-situ experiments, issue solving, combined techniques, automatic analysis software…
56/57

## Slide 57
Thank You
for your Attention!!!
Tae Joo Shin
tjshin@unist.ac.kr
PAL-XFEL
PLS-II
57/57