## Slide 1: Fundamentals and Advances in Superconducting Accelerator Magnets
徐庆金 Qingjin Xu
中国科学院高能物理研究所
Institute of High Energy Physics,
Chinese Academy of Sciences
超导加速器磁体基础及前沿进展
The 4th Asian School on Superconductivity Cryogenics for Accelerators (ASSCA2022)，
Korea University，Sejong Korea, Feb 13-19 2023

## Slide 2: Outline
Fundamental Principles of the Superconducting Accelerator Magnets
PRINCIPLES of Superconductivity and Particle Accelerators
CHARACTERISTICS and MAIN CHALLENGES of the Superconducting Accelerator Magnets
Case Study
Progress of the High Field Magnet R&D at IHEP
Progress of the HL-LHC CCT Magnets

## Slide 3: Outline
Fundamental Principles of the Superconducting Accelerator Magnets
PRINCIPLES of Superconductivity and Particle Accelerators
CHARACTERISTICS and MAIN CHALLENGES of the Superconducting Accelerator Magnets
Case Study
Progress of the High Field Magnet R&D at IHEP
Progress of the HL-LHC CCT Magnets

## Slide 4: Acknowledgement
The materials of this section are based on the following references
“Superconducting Accelerator Magnets” by Steve Gourlay and Soren Prestemon (LBNL), June 2018
“Superconducting Accelerator Magnets” by Soren Prestemon (LBNL), Paolo Ferracin and Ezio Todesco (CERN), June 2015
“Applied Electromagnetism: Magnet and RF-Cavity Design” by Mau Lopes and Jeremiah Holzbauer (FNAL), January 2016
USPAS website: http://uspas.fnal.gov/materials/materials-table.shtml
And talks from Lucio Rossi, Steve Gourlay et al, and the textbooks:
  Martin N. Wilson, "Superconducting Magnets", 1983.
  K.-H. Mess, P. Schmuser, S. Wolff, “Superconducting accelerator magnets”, Singapore: World Scientific, 1996.
  Fred M. Asner, "High Field Superconducting Magnets", 1999.

## Slide 5
The Discovery of Superconductivity
Successfully liquefied He gas
in 1908
Heike Kamerlingh Onnes
Dutch Physisist
(1853-1926)
The Nobel Prize in
Physics 1913
Heike Kamerlingh Onnes
"for his investigations on the
properties of matter at low
temperatures which led, inter alia,
to the production of liquid helium”
Discovery of Superconductivity in 1911
Temperature (K)
Resistance
5
Fundamentals & advances in superconducting magnets, QXU，Feb 2023

## Slide 6
传统超导体
(Tc < 40K)
Before 1986
铜氧化合物
高温超导体
(Tc 达160K)
1986/1987
铁基
高温超导体
(Tc 达55K)
2008
The History of Superconductors
Huiqian Luo
6
Fundamentals & advances in superconducting magnets, QXU，Feb 2023

## Slide 7
Basic Characteristics of Superconductors
第一类超导体
第二类超导体
Critical
Temperature
Zero Resistance
Meissner Effect
Jc vs Tc & Bc
Jc vs ε
Tc
Bc
7
Fundamentals & advances in superconducting magnets, QXU，Feb 2023

## Slide 8: PRINCIPLES of a Circular Collider
Lucio Rossi

## Slide 9: The 1st Superconducting Accelerator in the World
IEEE Milestone Award: The first large-scale use of superconducting magnets enabled the construction of the Tevatron. Established the superconducting wire manufacturing infrastructure that made applications such as Magnetic Resonance Imaging (MRI) viable.
Tevatron accelerator at Fermilab. Construction completed in 1980s.
774 superconducting NbTi dipole magnets + 240 NbTi quadrupole magnets

## Slide 10: The Largest Application of Superconductivity so far: LHC
1232 SC dipoles–15 m –8.33 T. 500 SC Quadrupoles. 8000 Corrector Magnets.
16 SC Cavities. 40 pairs large Current Leads in HTS
Lucio Rossi

## Slide 11: Hadron Colliders in the Past and Future
SPPC
FCC

## Slide 12: Dipole vs. Solenoid
Different coil configurations
Limited coil width for dipole
Magnetic shielding
Cost
Martin Wilson
Solenoid
Lucio Rossi
LHC dipole
Dipole
Je – Current density
t – Coil thickness
Je – Current density
t – Coil thickness

## Slide 13
Cos-theta dipole
Highest efficiency, complicated ends with hard-way bending
Common coil dipole
Simplest structure with large bending radius, lower efficiency
Canted cos-theta dipole
Lowest stress level in coil, lowest efficiency
Efficiency, field quality, stress management, quench protection…
Block type dipole
Simpler structure with hard-way bending, lower efficiency
Coil Configurations for Dipole Magnets

## Slide 14: The Dipole Magnets in Past Years
Tevatron
HERA
SSC
RHIC
LHC

## Slide 15: New Record：14.5 T Dipole by Fermilab

## Slide 16: Field Harmonics
From M. N. Wilson, pg. 28
An ideal cos
A practical winding with one layer and wedges
[from M. N. Wilson, pg. 33]
A practical winding with three layers and no wedges
[from M. N. Wilson, pg. 33]
Artist view of a cos magnet
[from Schmuser]
  Cos: a current density proportional to cos in an annulus - it can be approximated by sectors with uniform current density
Perfect Dipole
Biot-Savart law

## Slide 17: Field Harmonics
  Perfect quadrupole
  Cos2, a current density proportional to cos2 in an annulus- approximated by sectors with uniform current density and wedges
  (Two) intersecting ellipses
    Perfect sextupoles: cos3 or three intersecting ellipses
    Perfect 2n-poles: cosn or n intersecting ellipses
Quadrupole as an ideal cos2
Quadrupole as two intersecting ellipses
17
Fundamentals & advances in superconducting magnets, QXU，Feb 2023

## Slide 18: Field Harmonics
Maxwell equations for magnetic field
In absence of charge and magnetized material
and for 2D constant longitudinal field,
James Clerk Maxwell,
Scottish
(13 June 1831 – 5 November 1879)
Gauss's law for magnetism
Ampère's circuital law
A dipole
A quadrupole
[from P. Schmuser et al, pg. 50]
A sextupole

## Slide 19: Field Harmonics
Iron saturation effect: shaping the iron – the RHIC dipole
    The field in the yoke is larger on the pole
    Drilling holes in the right places, one can reduce saturation of b3 from 40 units to less than 5 units (one order of magnitude), and to correct also b5
19
Fundamentals & advances in superconducting magnets, QXU，Feb 2023

## Slide 20: Electro-magnetic Force
The e.m. forces in a dipole magnet tend to push the coil
- Towards the mid-plane in the vertical-azimuthal direction (Fy , F < 0)
- Outwards in the radial-horizontal direction (Fx , Fr > 0)
Tevatron dipole

## Slide 21: Electro-magnetic Force
LHC dipole at 0 T LHC dipole at 9 T
Usually, in a dipole or quadrupole magnet, the highest stresses are reached at the mid-plane, where all the azimuthal e.m. forces accumulate (over a small area).
Displacement scaling = 50

## Slide 22: Electro-magnetic Force
The e.m. forces in a quadrupole magnet tend to push the coil
Towards the mid-plane in the vertical-azimuthal direction (Fy, F < 0)
Outwards in the radial-horizontal direction (Fx, Fr > 0)
TQ

## Slide 23: Electro-magnetic Force
In the coil ends the Lorentz forces tend to push the coil Outwards in the longitudinal direction (Fz > 0)
Similarly as for the solenoid, the axial force produces an axial tension in the coil straight section.

## Slide 24: Electro-magnetic Force
Nb-Ti LHC MB (values per aperture)
  Fx = 340 t per meter
    ~300 compact cars
    Precision of coil positioning: 20-50 μm
  Fz = 27 t
    ~weight of the cold mass
Nb3Sn dipole (HD2)
  Fx = 500 t per meter
  Fz = 85 t
  These forces are applied to an object with a cross-section of 150x100 mm !!!
    and the material is brittle!

## Slide 25: Superconducting Materials
Discovered in 1911 by Kammerling-Onnes, observed that the resistance of a mercury wire disappeared at 4.2 K.
Nb3Sn and Nb-Ti, discovered in 1954 and 1961, are the most commonly used type II superconductors, suitable for practical application .
The critical temperature Tc is 9 K for NbTi and 18 K for Nb3Sn at 0 T, they are defined as low temperature superconductors (LTS).
Discovered from 1986, High temperature superconductors (HTS) have a Tc of up to 40-120 K.
by L. Bottura
B<Bc1
Bc1<B<Bc2
Type II superconductors

## Slide 26
By PJRay - Own work, CC BY-SA 4.0, https://commons.wikimedia.org/w/index.php?curid=46193149
Timeline of Superconducting Materials

## Slide 27: Nb-Ti vs Nb3Sn
critical surface : B (T), J (A/mm2), T (K)
Nb-Ti
Nb3Sn

## Slide 28: Copper vs Superconductors
Typical operational conditions (0.85 mm diameter strand)
Cu
Nb3Sn
Nb-Ti
Je ~ 5 A/mm2
I ~ 3 A
B = 2 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 8-9 T
Je ~ 600-700 A/mm2
I ~ 300-400 A
B = 12-13 T

## Slide 29: Superconductors for Accelerator Magnets
The superconductors for accelerator magnets should
  subdivided in filaments of small diameters
    to reduce flux jumps
    to minimize field distortions due to magnetization
  twisted together
    to reduce inter-filament coupling and AC losses
  embedded in a copper matrix
    to protect the superconductor after a quench
    to reduce flux jumps
NbTi LHC wire (A. Devred)
Nb3Sn bronze-process wire (A. Devred)
NbTi SSC wire (A. Devred)
Nb3Sn PIT process wire (A. Devred)

## Slide 30: Flux Jumps
  An external magnetic field penetrates in a type-II superconductor in the mixed state through fluxoids.
  If the superconductor is subjected to a thermal disturbance, the local change in Jc produces a motion or “jump” of fluxoids, which is accompanied by power dissipation.
  The stability criteria for a slab in the adiabatic condition
  where a is the half-thickness of the slab, jc is the critical current density [A m-2],  is the density [kg m-3], C is the specific heat [J kg-1], and c is the critical temperature.
  Nb-Ti filament diameters are usually less than 50 µm.
  High conductivity copper reduces instability.

## Slide 31: Hysteresis of the Magnetization
  Field distortions are proportional to rf. LHC filament diameter 6-7 µm; HERA filament diameter 14 µm.
From A. Jain, USPAS 2007, Dynamic effects in superconducting magnets, pg. 18

## Slide 32: Interfilament Coupling
  When a multi-filamentary wire is subjected to a time varying magnetic field, current loops are generated between filaments.
  If filaments are straight, large loops are generated, with large currents
    Big losses
  If the strands are magnetically coupled the effective filament size is larger
    Flux jumps
  To reduce these effects, filaments are twisted with a twist pitch of the order of 20-30 times of the wire diameter.
M.N. Wilson

## Slide 33: Quench Protection and Stabilization
  Superconductors have a very high normal state resistivity. A filament of Nb-Ti, if quenched in free space, could reach very high temperatures in few ms.
  If the filament is embedded in a copper matrix, when quench occurs, the current redistributes in the low-resistivity matrix and the peak temperature can typically be maintained below 300 K.
  The copper matrix facilitates quench protection: it allows the quench to propagate and it provides time to act on the power circuit.
  In the case of a small volume of superconductor heated beyond the critical temperature (for instance because of a flux jump), the current can flow in the copper for a short moment, allowing the filament to cool-down and recover superconductivity.
    The matrix also helps stabilizing the conductor against flux jumps (dynamic stability).

## Slide 34: Superconducting Cables
Most of the superconducting coils for particle accelerators are wound from a multi-strand cable.
The advantages of a multi-strand cable are:
  reduction of the strand piece length;
  reduction of number of turns
    easy winding;
    smaller coil inductance
      less voltage required for power supply during ramp-up;
      after a quench, faster current discharge and less coil voltage.
  current redistribution in case of a defect or a quench in one strand.
The strands are twisted to
  reduce inter-strand coupling currents
    Losses and field distortions
  provide more mechanical stability
The most commonly used multi-strand cables are the Rutherford cable and the cable-in-conduit.
A. Devred

## Slide 35
AC losses
Hysteresis: Reduce deff
Coupling: Reduce twist pitch; Modify inter-filament resistance
Eddy currents: laminations

## Slide 36: Fabrication of NbTi wires
The copper to superconductor ratio is specified for quench protection.
The filament diameter is chosen to minimize flux jumps and field errors due to persistent currents.
The inter-filament spacing is kept small for drawing operation, and large enough to prevent filament couplings.
A copper core and sheath is added to reduce cable degradation.
A. Devred

## Slide 37: Fabrication of Nb3Sn wires
Reaction of a PIT wire
A. Godeke

## Slide 38: Fabrication of Rutherford cable
The final shape of a Rutherford cable can be rectangular or trapezoidal.
The cable design parameters are:
  Number of wires Nwire
  Wire diameter dwire
  Cable mid-thickness tcable
  Cable width wcable
  Pitch length pcable
  Pitch angle cable (tan cable = 2 wcable / pcable)
  Cable compaction (or packing factor) kcable
Typical cable compaction: from 88% (Tevatron) to 92.3% (HERA).

## Slide 39: Fabrication of Coils for Accelerator Magnets

## Slide 40: Heat Reaction

## Slide 41: Quench
Analysis of SQ02, LBNL

## Slide 42: Quench Protection
Quench
Normal zone growth
Detection
Power supply switched off
Protection heaters
Extraction
Quenchback
Trigger protection options
Current decay in the magnet
Magnetic energy
Converted to heat

## Slide 43: Quench Protection
In most accelerator magnets, the “natural” resistance growth is insufficient to provide a good protection => Need to enhance the resistance
Method 1:
  Add an external resistor
Method 2:
  Protection heaters mounted on the coils
    Optimized to minimize thermal diffusion time
Method 3:
  Use of couple secondary circuits
    Can be external or internal to the coil
    Quench back
Method 4:
  Coil subdivision
Cold

## Slide 44: Quench Protection
Coupling-Loss Induced Quench Protection
CLIQ
E. Ravaioli et al.
G. Kirby et al.
METROSIL Quench Protection

## Slide 45: Quench Protection
In the LHC main ring, the dipoles are connected in series. The principle is
  to “by-pass” the quenching magnet to avoid dumping all the string energy in one magnet
  To de-excite the rest of the magnets into a dump resistor
Combination of various methods: heaters, dump resistor, diodes

## Slide 46: Training
Training is characterized by two phenomena
  The occurrence of premature quenches
    Frictional motion of a superconductor
    Epoxy failure
    ……
  The progressive increase of quench current
    Some irreversible change in the coil’s mechanical status.
In R&D magnets, training may not be an issues.
For accelerator magnets it can be expensive, both in term of time and cost.

## Slide 47: Quench Origins
  Depending on the shape of the voltage signal, it is possible to identify
    Conductor limited quenches: slow, gradual resistive growth
    Flux jump induced quenches: low-frequency flux changes
    Motion induced quenches: acceleration-deceleration-ringing
Conductor limited
Flux-Jump
Motion

## Slide 48: Modeling from magnets to filaments
D. Arbelaez et al, “Cable Deformation Simulation and a Hierarchical Framework for Nb3Sn Rutherford Cables,” EUCAS, pp. 1–11, 2009
A. Godeke

## Slide 49
Precondition (Iron based conductor, ReBCO, Bi-2212,…)
The Je of the HTS conductors is high enough for accelerator application
The cost is lower than or similar with the LTS conductors
Mechanical performance is qualified
Main challenges of the HTS technology
Quench protection：quench propagation speed of HTS conductors is about two orders of magnitude lower than the LTS case
Cable fabrication：how to fabricate high-current cable with tapes?
Coil layout：compact, high efficiency, stress control, …
Field quality control：10-4 field uniformity needed for accelerators
Advantages of the all-HTS magnet：
Possibility of raising the operation temperature of the magnet（4.2K -> ?K）
HTS 16+ Tesla Accelerator Magnet?

## Slide 50: Outline
Fundamental Principles of the Superconducting Accelerator Magnets
PRINCIPLES of Superconductivity and Particle Accelerators
CHARACTERISTICS and MAIN CHALLENGES of the Superconducting Accelerator Magnets
Case Study
Progress of the High Field Magnet R&D at IHEP
Progress of the CCT Magnets for HL-LHC

## Slide 51
Cabling Coil winding HT VPI Magnet assembly Test
Tension control, deformation
Jc and RRR degradation,
Flux jump…
Stress control,
Size control,
Electrical insulation
Jc and Field quality
degradation,
Electrical short…
Temperature control,
Thermal stress control
Jc and RRR degradation.
Impregnation quality control: type of epoxy, procedures;
Mechanical strength and stability
Pre-stress control
Stress of coils,
Mechanical
Stability…
EM force, Quench protection
Training,
Strain of coils…
Material, Structure, Processing,…
Jc, RRR, Cu ratio,
Filament size…
Fabrication Steps of the High Field Accelerator Magnets
51

## Slide 52
High Field Model Dipole Magnet: 12.47T @ 4.2K
Picture of LPF1-U

## Slide 53
The cross-section of LPF3
Coil layout (yoke 1/8)
OD:640 mm
120 mm
AP:30 mm
Field and flux distribution in coils
58
42
58
24
54
24
50
20
1
2
3
4
5
6
Main field: 16 T
Nb3Sn
YBCO
Nb3Sn
LTS (13 T) + HTS (3 T)
Current | 7580/143 A |  | Blocks | Block 1 | Block 2 | Block 3 | Block 4 | Block 5 | Block 6 | Block 7
Main field | 16.03 T |  | Peak field (T) | 12.81 | 10.68 | 10.82 | 10.58 | 10.48 | 10.38 | 16.18
 |  |  | LL ratio (%) | 77.66 | 75.61 | 77.56 | 76.15 | 78.45 | 77.87 | -
Peak field | 16.74 T |  | Blocks | Block 8 | Block 9 | Block10 | Block11 | Block12 | Block13 | Block14
 |  |  | Peak field (T) | 15.98 | 16.18 | 15.95 | 16.64 | 16.25 | 16.74 | 16.56
Harmonics | Max: 5.27 U |  | b3: -4.4 | b5: -5.27 | b7: -0.3 | b9:-1.62 | a2:-1.15 | a4: 2.77 | a6:-0.95 | a8:-0.15
Main parameters of LPF3
High Field Model Dipole Magnet: 16-T Design

## Slide 54
Block with SC
The angle between the flux direction and the tape wide surface has been optimized
Harmonics | b3 | b5 | b7 | b9 | a2 | a4 | a6 | a8
Unit | -3.2 | -7.7 | -3.8 | -0.9 | 0.9 | -5.5 | -2.5 | -0.6
High Field Model Dipole Magnet: 16-T Design

## Slide 55
Magnet structure
Stress distribution in different loading steps
After assembly at RT: Peak stress on shell- 128 Mpa; On rod- 468 Mpa; On coils- 28.1 Mpa
Cooling down at 4.2 K: Peak stress on shell- 215 Mpa; On rod- 618 Mpa; On coils- 72.3 Mpa
Excited to 13 T: Peak stress on shell- 218 Mpa; On rod- 612 Mpa; On coils- 93 Mpa
High Field Model Dipole Magnet: 16-T Design

## Slide 56
A simplified circuit was established in COMSOL
A 1-dimensional adiabatic model was established
Varistor and heaters are applied to the quench protection of LPF3
Simplified circuit
 | Thickness of stainless steel /μm | Resistance/Ω | Power（W/cm^2) | Charging voltage/V | Resistivity
coil1 | 50 | 2.505 | 50 | 389.76 | 0.5μΩ·m
coil2 | 100 | 1.698 | 50 | 339.6 | 
coil3 | 100 | 1.878 | 50 | 375.6 | 
Parameter of heaters
Main parameter of the magnet
Heaters
Temperature distribution near hot spots
The calculation indicates that the temperature of hot spot is 237 K and the max voltage is 952 V. Safe.
High Field Model Dipole Magnet: 16-T Design

## Slide 57
Nb3Sn Rutherford cable fabrication
Coil fabrication
Heat treatment test
Inner splice soldering
Pre-assembly
Nb3Sn Rutherford cable has been fabricated for LPF3
A dummy coil has been fabricated and heat treated to test the furnace property
The inner joints fabrication test and the pre-assembly of LPF3 has been carried out.
The coils of LPF3 is under construction and the fabrication of the LPF3 is expected to be competed in mid 2023.
High Field Model Dipole Magnet: 16-T Fabrication

## Slide 58
High lights:
Canted-Cosine-Theta (CCT) technology;
  Superior field quality;
  Stress management
  Developed industrial assembly line;
Graded Nb3Sn Rutherford cables;
Multiple replaceable coil modules;
The geometry of the 4 module CCT magnet
BI
BO
BM
Ribs
Spar
CCT subscale
High Field Model Dipole Magnet: 16-T CCT option
At 4.2 K, the magnet produces 16 T at 100% load-line with 8.8 kA operating current

## Slide 59
Harmonics： 10-4 | b2 | a2 | b3 | a3 | b4 | a4 | b5 | a5 | b6 | a6 | b7 | a7 | b8 | a8
Cross section-2D | 0.6259 | 0.0119 | 2.9824 | -0.0006 | 0.0537 | 0.0002 | 0.5189 | 0.0002 | 0.0183 | -0.0020 | -0.0845 | 0.0016 | -0.0036 | 0.0009
Integrated-3D | 1.5989 | 0.0101 | 3.8649 | -0.0320 | 0.3047 | 0.0802 | 1.4069 | -0.0175 | 0.0750 | -0.3695 | 0.1163 | 0.0734 | -0.0223 | -0.2090
The CCT magnet has an intrinsic good field quality
High-order harmonics along axis - Bn
High-order harmonics along axis - An
High Field Model Dipole Magnet: 16-T CCT option

## Slide 60
Time chart of research progress of transposed cables
Cable design
Schematic illustration of the transposed cable and the fabrication steps
The advantages of the designed cable:
High current-carrying compacity
Low dynamic loss
High mechanical stability
High Field Model Dipole Magnet: HTS Cable R&D
In-plane bending performance of the REBCO tapes
J. Wang et al, Superconductivity 3 (2022) 100019

## Slide 61
IBS transposed cable
REBCO transposed cable
strand
cable
heat treatment
Terminal fabrication
test
The measured V-I curves of the IBS transposed cable
10-m cable samples bas been fabricated
Most of the tapes extracted from the cable showed almost no degradation.
Cable current reached ~2000 A
High Field Model Dipole Magnet: HTS Cable R&D

## Slide 62
2008.02
2008.09
2016
2018
Discovery of IBS
2008.04
Discovery of
122 phase IBS
2020
100-m 7-core IBS tape fabricated
IBS solenoid at 24 T
Racetrack at 8 T
The engineering current density of the long-length IBS still needs a significant improvement, to reach the similar level as ReBCO or Bi-2212 conductors.
The materials of stabilizer should be shifted to copper or any other low-cost metals to realize the low cost of IBS.
Structure and fabrication methods of IBS and corresponding coils should be further optimized to minimize the Jc degradation at high field and high stress.
And many other issues like detailed magnetic and mechanical properties study of IBS, quench detection and protection of the IBS coils / magnets and etc.
IBS solenoid at 32 T
Racetrack at 10 T
2022
IBS Technology: Status and Outlook
H. Hosono
IBS (Tc 26K)
Z. Zhao
IBS (Tc 55K)

## Slide 63
IBS Technology: Status and Outlook
Chart: Applied Magnetic Field (T)
| 0 | 5 | 15 | 20 | 25 | 30
REBCO: B ∥ Tape plane | 4144.6766 | 3507.9375 | 3148.3332 | 2909.0554 | 2090.4933 | 1888.9952
REBCO: B ⊥ Tape plane, 45 μm sub | 5478.1345 | 5053.3515 | 4372.0346 | 3812.2534 | 3348.8068 | 3146.724 | 2964.7726 | 2801.365 | 2663.2305 | 2530.35 | 2415.161 | 2307.3222 | 2215.5971 | 2121.427 | 2046.7953 | 1970.1838 | 1905.1216 | 1841.6283 | 1784.4676 | 1729.8653 | 1682.3664 | 1631.1403 | 1591.3007
REBCO: B ⊥ Tape plane | 4144.6766 | 1445.8386 | 975.0997 | 767.7508 | 655.6687 | 571.6114 | 526.7777 | 481.944 | 442.7183 | 428.1462 | 403.4904 | 386.6773 | 364.2626 | 341.8457 | 328.3952 | 319.4289 | 318.3073
Bi-2212: OST NHMFL 50 bar OP | 1243.4169 | 1159.7904 | 1097.571 | 1051.5861 | 1014.8275 | 981 | 955.0755 | 928.7776 | 905.6283 | 884.9933 | 865.478 | 846.7181 | 827.3047
Nb₃Sn: Internal Sn RRP® | 1754.8557 | 1454.9349 | 1190.9814 | 1072.6374 | 957.7741 | 855.0933 | 757.6336 | 268.0143 | 190.8587 | 118.9241 | 65.5533 | 28.3097
Nb₃Sn: High Sn Bronze | 166.6431 | 137.8146 | 111.0954 | 84.3762 | 60.8212 | 40.0788 | 19.3362 | 8.0861
Nb-Ti: LHC 4.2 K | 5106.8846 | 4054.1538 | 3180.5962 | 2710.2269 | 2217.4577 | 1724.6885 | 1411.1115 | 1187.1231 | 918.3423
Nb-Ti: Iseult/INUMAC MRI 4.22 K | 393.4783 | 291.3043 | 194.203 | 104.3478
Exponential Y-axis Labels | 10 | 100 | 1000 | 10000
Nb-Ti midrange maximal | 971.9231 | 687.3077 | 448.4615 | 393.4783
2212 Fitted Line for 50bar ASC'16 | 1381.5217 | 1248.5735 | 1162.079 | 1099.1369 | 1050.2486 | 1010.6145 | 977.4929 | 949.1799 | 924.5486 | 902.818 | 883.4258 | 865.9547 | 850.0872 | 835.5764 | 777.6921 | 691.6232
YBCO B perp linear extrap | 312.7055 | 264.5487 | 240.4379
IBS 2019
IBS 2022
IBS 2025
Stainless-steel stabilized IBS tape achieved the highest Je in 2022!
Significantly reduced the cost and raised the
mechanical properties.

## Slide 64
First IBS Racetrack Coil at 10 T
Ic of Φ34mm-17 turns-DPC reached 60 A at 4.2 K and 32 T, a new breakthrough！
IBS Magnet R&D: High Field Model Coils
First IBS Solenoid Coil at 32 T
Zhang, et al., SuST,. 34 (2021) 035021
Two racetrack coils have been made using 100- m length Iron-Based Superconducting tapes.
The coils reached 86.7% of the Ic of the short sample at 4.2 K, 10 T, 81.25% of the quench current under self-field,
with highest compressive stress of 120 MPa.

## Slide 65
R&D Roadmap for next years
NbTi+Nb3Sn
2*ф10 aperture
10T @ 4.2K
Challenges: Fabrication process, stress control
year
2018
2028
Field
(T)
10
20
Nb3Sn+HTS
2*ф30 aperture
15T @ 4.2K
Challenges: Fabrication process, stress control, quench protection
Nb3Sn+HTS or HTS
2*ф45 aperture
20T @ 4.2K
With 10-4 field quality
Challenges: Stress control, quench protection, field quality control

## Slide 66
Development of CCT Dipole Magnets for HL-LHC
HL-LHC加速器升级中国贡献
China provides 12+1 units CCT twin-aperture dipole magnets for HL-LHC project
5Tm dipole field in the two apertures at 1.9K, To be installed in the ATLAS & CMS interaction regions.

## Slide 67
Fabrication of a full size prototype magnet MCBRDP2 was completed in May, 2020. Both apertures reached the ultimate current.
MCBRDP2
MCBRD02
MCBRD01
The first set of CCT superconducting magnets MCBRD01 with satisfactory field strength and field quality, has been shipped to Europe in October, 2021.
The assembly of the 2nd set of HL-LHC CCT superconducting magnets has been finished in Jan, 2022, passed the performance test at IMP in May, being shipped to CERN this month.
Development of CCT Dipole Magnets for HL-LHC

## Slide 68
Development of CCT Dipole Magnets for HL-LHC
2+10 apertures has been fabricated. Most of them reached design current, but with long training.
From CB09 an important modification to the design has been adopted, to improve the training performance of the CCT coils
CB09 & CB12 tested at IHEP shows excellent training performance, demonstrated the expected effect of the design upgrade.
CCT coils stand-alone test at IHEP
Design upgrade: times of training quench reduced by an order of magnitude
Successful design upgrade to solve the “long training problem”, significantly reduced the times of quench during training, ensured the project progress “on track”.
CCT Magnet under test at CERN

## Slide 69: Applications of the Superconductivity Technology
科学前沿
高能量粒子加速器
能源前沿
磁约束核聚变装置
精准医疗
先进MRI成像设备
先进交通
磁悬浮高速列车
清洁能源
超导发电
先进电力
低损耗电力输送
Thanks! Questions and Discussions……